## Slide 1: How to calculate breakage probability ?
If = no. of incident particles,
= no. of rebound particles,
= fraction of rebound particles generated from breakage, then
can be estimated from experimental PSD data of initial and rebound particles.

## Slide 2: Method to estimate from expt. data
If = CDF of incident particles (raw data available)
= CDF of rebound particles (raw data available)
= CDF of broken fragments (raw data not available)
There are two different ways we can fit and to find .
Assume some known distribution for both datasets (lognormal, polynomial, etc.) and find parameters of the functions that minimize the divergence from experimental data.
If above functions don’t work, use piecewise linear functions instead. Also called multivariable linear optimization. This approach is the benchmark.

## Slide 3: Multivariable linear optimization
diameter
diameter
diameter
Initial PSD
Rebound PSD
Broken PSD
function f =

## Slide 4: Multivariable linear optimization (Contd)
Optimization reduces to
Minimize function f = subject to the following constraints:
(k) <1 for k = 1,2,….n-1
(n) = 1
(k) < (k+1) for k = 1,2,…..n-1
where n = no. of CDF datapoints (16 for our case)

## Slide 5: Lognormal fitting
+

## Slide 6: (Lognormal + Polynomial) fitting
+

## Slide 7: Piecewise linear fitting
diameter
diameter
Initial PSD
Rebound PSD

## Slide 8
Approach A
Incident: log-normal fitting
Rebound: log-normal fitting

## Slide 9
Approach B
Incident: 5-order polynomial fitting
Rebound: log-normal fitting

## Slide 10
Approach C
Incident: piecewise linear
Rebound: piecewise linear
Typical optimization results
V = 103.4 m/s
= 30o
Bn = 0.324

## Slide 11
volume of visible particle
volume of incident
= g = 1.0
volume of visible particle
volume of incident
= g = 0.5
Approach C – consider the mass loss to invisible rebound particles
Incident: piecewise linear
Rebound: piecewise linear

## Slide 12: Backup data – piecewise linear CDF of incident, rebound, and broken particles

## Slide 13: Results of predicted PSD
Speed OP1, angle 20 degrees
Speed OP1, angle 30 degrees

## Slide 14: Results of predicted PSD
Speed OP1, angle 40 degrees
Speed OP1, angle 50 degrees

## Slide 15: Results of predicted PSD
Speed OP1, angle 60 degrees
Speed OP1, angle 70 degrees

## Slide 16: Results of predicted PSD
Speed OP1, angle 80 degrees
Speed OP1, angle 90 degrees

## Slide 17: Results of predicted PSD
Speed OP2, angle 20 degrees
Speed OP2, angle 30 degrees

## Slide 18: Results of predicted PSD
Speed OP2, angle 40 degrees
Speed OP2, angle 50 degrees

## Slide 19: Results of predicted PSD
Speed OP2, angle 60 degrees
Speed OP2, angle 70 degrees

## Slide 20: Results of predicted PSD
Speed OP2, angle 80 degrees
Speed OP2, angle 90 degrees

## Slide 21: Results of predicted PSD
Speed OP3, angle 20 degrees
Speed OP3, angle 30 degrees

## Slide 22: Results of predicted PSD
Speed OP3, angle 40 degrees
Speed OP3, angle 50 degrees

## Slide 23: Results of predicted PSD
Speed OP3, angle 60 degrees
Speed OP3, angle 70 degrees

## Slide 24: Results of predicted PSD
Speed OP3, angle 80 degrees
Speed OP3, angle 90 degrees